Bond tests on Printed Circuit Boards with Palladium Metallizations

Ian Mcgill and Christian Joram – PH/TA1/SD

May 2004

Bond tests were performed on two PCB samples fabricated by the French company CIRLY. The samples feature Copper (Cu) soldering pads, which are electrolytically coated with a 0.2 m thick layer of Palladium (Pd). Some information on the advantages of Palladium is given in the annex at the end of this document.

Bond equipment:

Delvotec 6400 aluminium wedge bonder(45deg feed angle), tool 4W4F-1820-W7C_F00, wire 25micron Al/1%Si, US frequency 100 kHz

Testing equipment:

Wire pull tester, Dage type 2400A, geometry 30degree pull on 1st and 2nd bonds. The bondwire length was 1.5mm.

Performed tests:

3 sets of bond tests with 10 wires each were made changing the following parameters

| Parameter | Set.1 | Set.2 | Set.3 |
| --- | --- | --- | --- |
| Ultrasonic Power | 75 | 70 | 75 |
| Bond Force | 125 | 100 | 100 |
| Touch Down Force | 115 | 90 | 90 |
| US Power Max. | 20 | 20 | 20 |
| US Power Min | 75 | 70 | 75 |

The following relevant parameters were kept constant for all sets.

| Parameter | value |
| --- | --- |
| Deformation | 70 |
| Rampsteps | 250 |
| Bond delay | 20ms |
| Touch down delay | 10ms |
| Curvescale | 1150 |
| TD Delay | 10ms |
| Td Offset | 20 |
| TD Steps | 2 |

The statistical analysis gave the following results.

Set.1 Set.2 Set.3

Min: 10.41 10.45 10.13

Mean: 10.70 10.86 10.498

Max: 10.97 11.21 10.73

Std Dev.: 0.206 0.252 0.254

The 3 parameter sets give good pull tests results. The failure mode is in practically all cases ‘First heel failure’ as it should be. Set 1 is believed to give the best results in terms of surface variability.

Some tests were carried out using a lower deformation of 65. This also gave good results, but to allow for surface variability and flaws the slightly higher deformation should be more consistent.

Further tests

2 sets of bond tests with 10 wires each were made changing the following parameters

| parameter | Set.4 | Set.5 |
| --- | --- | --- |
| Ultrasonic Power | 75 | 75 |
| Bond Force | 140 | 125 |
| Touch Down Force | 130 | 115 |
| Us Power Max | 20 | 15 |
| Us Power Min | 75 | 75 |

Set.4 failure modes: 6 x Second Bond Lift, 1 x Midwire Break, 3 x First Heel Failure

Set.5 failure modes: 2 x Second Bond Lift, 2 x Midwire Break, 5 x First Heel Failure

The statistical analysis gave the following results:

Set.4 Set.5

Min: 7.61 10.33

Mean: 9.37 10.87

Max: 10.85 11.37

Std Dev.: 1.28 0.318

Conclusion

Palladium coated Copper pads can be used for Aluminum wedge bonding, leading to good pull test results.

Characterization of long term reliability and behavior under special environmental conditions, e.g. high or low temperature or strong temperature variations, would require further more extensive tests.

Annex : Palladium

PRINCIPLE: Electrolytic plating of Palladium ( Pd) on copper. Thickness of the plating env. 0,2µm. ADVANTAGES: QUALITY Finish particularly adapted to circuits classifies 5 Good flat deposit specially useful for the soldering of SMD Good wetability, good soldering, beautiful aspect Mastery of a process which is perfectly integrated into our workshop Abolition of the lead (protection of the environment) The palladium plating is practised within weak temperatures: abolition of the thermic shocks related to the HAL Compatibility with the various types of soldering pastes excellent definition of etching Very good behaviour within the etching Does not oxidize below 400degC DELAY : Saving of time Mastery of the process internally Reliability of the delay still increased INCONVENIENCES: Palladium is a noble metal Its rate is fluctuating CHARACTERISTICS: TECHNOLOGICAL Flat plating and soudable very fine plating < or = to 0,2µm directly on the copper Allows SMD with the finest pitches which one can find today Allows the Chip On Board gold and aluminium wire systems to be used Process already used in the finish of the components. PHYSICS Hardness = 240-260 Knoop Density = 11,5-12,0 g / cm3 Internal tension= 62-64 KPSI Strain = > 6 % Structure = Equiaxiale with fine grain Dissolution of the Pd at 250°C during 3 seconds Copyright© CIRLY S.A. 2001 - Design by FORNEXT

# Footnotes

CIRCLY SA, Lyon, France. www.cirly.com

All numbers are machine specific and will be different on other bonding machines

All numbers are machine specific and will be different on other bonding machines